## Slide 1: 博士学位答辩 硅基超构多维光场调控
答辩人：赵耀天
指导老师：郭旭涵 教授
上海交通大学区域光纤通信网与新型光通信系统国家重点实验室

## Slide 2
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望

## Slide 3
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望

## Slide 4
新兴技术的涌现-大容量信号传输的更高要求
新兴技术的涌现对大容量信号传输提出更高要求
亟需高速率、大带宽、低功耗的数据处理与传输技术
智能驾驶
人工智能
超算中心

## Slide 5
新兴技术的涌现-大容量信号传输的更高要求
新兴技术的涌现对大容量信号传输提出更高要求
亟需高速率、大带宽、低功耗的数据处理与传输技术
数据量快速增长
摩尔定律放缓
R. Chen, et al., Int. J. Extreme Manuf. , 2, 022002 (2020).

## Slide 6
集成光子芯片技术-高速互连极具潜力的解决方案
集成光电子技术有潜力在芯片上低成本实现高速的光互连
S. Y. Siew, et al., J. Light. Technol. 39, 4374–4389 (2021).
集成光电子器件的功能:
在芯片上实现光的互连、处理、调制和探测等功能器件
集成光电子芯片的优势：
与CMOS兼容
低损耗
低功耗
高集成度
大带宽
……
From Intel

## Slide 7
多维光复用技术-进一步增加光互连的通信容量
D. Dai, J. Wang, S. Chen, S. Wang, and S. He, Laser Photonics Rev. (2015).
多维光复用


精准调控和高效耦合
高集成度和大通量
2偏振× M模式×N波长
通过多种维度（偏振、模式、波长）来复用光信号，可以进一步提高通信容量，满足日益增加的通信容量需求

## Slide 8
超构材料 - 强大的片上光场调控能力
传统光学器件
空间光超构表面器件
From Samsung
Zhao, R., et al., PhotoniX 1, 20 (2020)
片上超构材料器件
Y. Zhang, et al., ACS Photonics 17, 43 (2020).
J. Xiang, Y. Zhao, X. Guo,* et al., . Light: Science & Applications 11, 168 (2022).
超构材料提供自由设计的折射率分布，影响光场的传播过程中的相位分布，实现强大的片上光场调控能力

## Slide 9
超构材料 - 设计各种高性能光学器件
超构材料赋能实现更紧凑、更大带宽、更多功能的片上光学器件，展现出很大的研究前景

## Slide 10
主要研究工作

## Slide 11
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望

## Slide 12
耦合模理论 – 研究模式之间的耦合和转化
光在波导中以模式的形式进行传播
波导中传播的电磁波可以被分解为不同的本征模

## Slide 13
耦合模理论 – 电介质微扰引起的模式转化
电介质微扰 -> 耦合系数
耦合过程：耦合模方程
电介质微扰的设计
（均值为0的周期函数）
周期的耦合系数可以补偿模式之间的相位失配
超材料微扰引入了等效动量来弥补相位失配

## Slide 14
耦合模理论方法的应用形式
两根波导间不同模式的同向耦合
一根波导中不同模式的同向耦合
两根波导间不同模式的反向耦合
一根波导中不同模式的反向耦合

## Slide 15
有效介质理论 – 等效折射率
SiO2
Si
SiO2
neq
Y. He, Y. Su, et al., J. Light. Technol. 36, 5746 (2018).
有效介质理论将亚波长周期结构等效为具有统一折射率的均匀材料，用来计算微纳结构的光学特性

## Slide 16
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望

## Slide 17
片上偏振多样性系统的应用
偏振态是波导模式本质特性，在通信、计算、传感等领域具有广泛的应用
Y. Zhao, X. Guo,*, et al., Laser & Photonics Reviews, no. 2300320, 2023.

## Slide 18
设计原理
模式展开：
反向耦合：
同向耦合 (偏振旋转)

## Slide 19
设计原理-起偏器
周期的耦合系数可以补偿模式之间的相位失配
周期的微扰提供一个周期性的耦合系数
器件原理
器件结构

## Slide 20
设计原理-起偏器
损耗 < 0.3 dB
串扰 > 30 dB
带宽 > 200 nm
仿真结果
器件结构
TM入射光
TE入射光

## Slide 21
设计原理-偏振分束器
入射光首先被分解到不同模式的光，
通过反射光的相位来控制光的输出端口路径
仿真结果
器件结构

## Slide 22
设计原理-偏振分束器
仿真结果
器件结构
损耗 < 1 dB
串扰 > 30 dB
带宽 > 50 nm

## Slide 23
设计原理-偏振分束旋转器
器件原理
器件结构

## Slide 24
设计原理-偏振分束旋转器
基于电介质槽的模式解复用器
器件原理
器件结构

## Slide 25
设计原理-偏振分束旋转器
损耗 < 0.5 dB
串扰 > 14 dB
带宽 > 80 nm
仿真结果
器件结构

## Slide 26
仿真结果总结
起偏器
偏振分束器
偏振分束旋转器
Loss < 1.2 dB Crosstalk < − 30 dB Length: 18 μm
Loss < 0.6 dB Crosstalk < − 30 dB
Length: 16 μm
Loss < 0.7 dB Crosstalk < − 12 dB
Length: 13 μm
通过电介质微扰的方式，在片上实现了超紧凑、高性能的起偏器、偏振分束器、偏振分束旋转器

## Slide 27
加工和测试
起偏器
偏振分束器
偏振分束旋转器
Loss ≈ 1dB
Crosstalk < − 35 dB Length: 18 μm
Loss ≈ 2 dB
Crosstalk < − 30 dB
Length: 16 μm
Loss ≈ 1.3 dB Crosstalk < − 12 dB
Length: 13 μm

## Slide 28
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望

## Slide 29
片上模分复用系统的应用
携带不同信号光，可以用不同的模式在一根波导中同时传播，从而增加了在单波长下的通道数，进而有效增加通信容量。
模分复用系统
L. W. Luo, M. Lipson et al., Nat. Commun. 5, 1–7 (2014).
J. Wang, S. He, and D. Dai, Laser & Photonics Rev. 8, 18–22 (2014).

## Slide 30
片上模式 (解)复用器
器件结构
仿真电场分布
利用简单电介质槽，实现模式转化
不同端口输入TE0模式耦合到总线波导中不同的模式
设计原理
Y. Zhao, X. Guo* et al., ECOC 2020, Tu2B-4.
同相位的模场TE0模式，反相位的模场 TE1模式
定向耦合引入90°的相位延迟，上下波导宽度差引入额外90°的相位延迟
上面入射光->同相位的模场(−90°+ 90°) -> TE0模式
下面入射光->反相位的模场(+90°+ 90°) -> TE1模式
TE0
TE0
TE0
TE1

## Slide 31
片上模式 (解)复用器
损耗<0.64 dB
串扰<−12dB
尺寸: 1 ×1.8 μm2
带宽: 200 nm
仿真结果
实验结果
单端损耗< 0.5 dB
串扰<−10 dB
尺寸: 1 × 1.8 μm2

## Slide 32
比较与总结
结构 | 面积 (μm2) | 插入损耗(dB) | 串扰(dB) | 带宽(nm)
Y型分束器 [1] | 180×2 | 1.5 | −19 | 90
亚波长光栅辅助绝热耦合器[2] | 55×3 | 2.6 | −18.8 | 130
非对称定向耦合器[3] | 50×1.3 | 0.3 | −16 | 100
多模干涉器[4] | 7.24×1.5 | 2 | <−15 | 50
逆向设计的点阵结构[5] | 3×2.4 | 1 | −24 | 60
本工作 | 1.8×1 | 0.5 | −10 | 60
[1] Z. Zhang, Y. Yu, and S. Fu, IEEE Photonics J., vol. 9, no. 2, 2017.
[2] L. Xu et al., J. Light. Technol., vol. 37, no. 23, pp. 5790–5800, 2019.
[3] Y. Ding, J. Xu, F. Da Ros, B. Huang, H. Ou, and C. Peucheret Opt. Express, vol. 21, no. 8, p. 10376, 2013.
[4] Z. Wang, C. Yao, Y. Zhang, and Y. Su, 2020 Opt. Fiber Commun. Conf. Exhib. OFC 2020 - Proc., vol. 1, pp. 5–7, 2020.
[5] W. Chang et al., Opt. Express, vol. 26, no. 7, p. 8162, 2018.
我们设计的器件具有迄今为止最小的尺寸(1 ×1.8 μm2), 在损耗、带宽、串扰等其他方面的性能上也很有竞争力。

## Slide 33
片上模式转化器
仿真光谱响应
1.2 μm
损耗<1.2 dB、串扰<−20 dB、尺寸：0.8 ×1.2 μm2
理论计算
FDTD仿真和理论计算结果较为符合
器件结构
仿真电场分布
利用简单电介质槽，实现模式转化
输入TE0模式完全转化为TE1模式
Y. Zhao, X. Guo,* et al. Opt. Lett. 45, 3797-3800 (2020).

## Slide 34
片上模式转化器
工艺容忍度分析
介质槽宽度变化±10nm范围内，损耗始终小于1.2dB，串扰小于−20dB
实验方案
通过基于非对称定向耦合器(ADC)的模式解复用器检测波导中的模式
实验结果
损耗<1.2 dB 串扰<−6.3 dB 尺寸：0.8 ×1.2 μm2
迄今为止最小的尺寸(0.8 ×1.2 μm2)
向高阶模式的拓展性
良好的工艺容忍度(±10 nm)

## Slide 35
片上模式转化器
TE0-TE1:
仿真: 插损: <0.15 dB
串扰:<−20 dB
实验: 插损: <0.5 dB
串扰<−7 dB
TE0-TE2
仿真: 插损: <0.22 dB
串扰:<−18 dB
实验：插损: <0.3 dB
串扰<−9 dB
级联特性(TE0-TE3)
仿真：插损: <0.83 dB
串扰:<−10 dB

## Slide 36
比较与总结
结构 | 耦合长度(μm) | 插入损耗(dB) | 串扰(dB) | 带宽(nm) | 器件功能
条状电介质波导 [1] | 2.635/2.27 | 2.1/1.37 | −13.4/−12.6 | 45 | TE0-to-TE1/TE2
电介质超表面结构 [2] | 5.75/6.736 | <1 | <−10 | 20 | TE0-to-TE1/TE2
拓扑优化光子晶体[3] | 6.3 | 2 | −12 | 43 | TE0-to-TE1
逆向设计优化[4] | 4 | <2.3 | <−11.5 | 40 | TE0-to-TE1 & TM0- to-TM1
本工作 | 2.3/2.4 | 0.5/0.3 | −7/−9 | 50 | TE0-to-TE1/TE2
本工作 | 1.2 | 1.2 | −6.3 | 50 | TE0-to-TE1
1. B. E. Abu-Elmaaty, M. S. Sayed, R. K. Pokharel, and H. M. H. Shalaby, Appl. Opt. 58, 1763 (2019).
2. H. Wang, Y. Zhang, Y. He, Q. Zhu, L. Sun, and Y. Su, Adv. Opt. Mater. 7, 1801191 (2019).
3. L. H. Frandsen, Y. Elesin, L. F. Frellsen, M. Mitrovic, Y. Ding, O. Sigmund, and K. Yvind, Opt. Express 22, 8525 (2014).
4. H. Jia, H. Chen, J. Yang, H. Xiao, W. Chen, and Y. Tian, Opt. Lett. 44, 4179
迄今为止最小的尺寸(0.8 ×1.2 μm2)
向高阶模式的拓展性
良好的工艺容忍度(±10 nm)

## Slide 37
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望

## Slide 38
常见波长调控方案
马赫-曾德尔干涉仪 (MZI)
阵列波导光栅 (AWG)
微环谐振腔 (MRR)
尺寸小、损耗低，但FSR受限，频谱通常为洛伦兹形
性能良好，但尺寸较大且对分束比有着严格的要求
频谱形状好，但耦合长度和带宽之间互相制约
通道串扰较小，但尺寸、损耗较大
S. GUERBER, et al., Opt. Lett. 45, 6559–6562 (2020).
S. Wang, et al., Opt. Lett. 42, 2802 (2017).
H. Xu and Y. Shi, IEEE Photonics Technol. Lett. 30, 169–172 (2018).
亚波长光栅多模波导(MBG)
D. Liu, et al., IEEE Photonics Technol. Lett. 32, 192–195 (2020).

## Slide 39
超构材料单通道滤波器
器件结构
由模式解复用器和超构材料波导构成
浅刻蚀的微扰结构
周期的耦合系数可以补偿模式之间的相位失配
周期的微扰提供一个周期性的耦合系数
Y. Zhao, X. Guo* et al., Laser & Photonics Rev., 2200005, 2022.
设计原理

## Slide 40
超构材料单通道滤波器
不同波长的入射光会有不同的表现.
波长为1570nm的光完全透射，而波长为1550nm的光完全反射.
滤波器的频谱顶部较平，而下降的也很快.
损耗很低，小于0.2 dB.
通过切趾抑制了旁瓣，旁瓣抑制比>20dB.
仿真电场能量分布
仿真结果

## Slide 41
超构材料多通道滤波器
多通道的拓展结构
通过合理的设计微扰的位置，我们把结构向多通道进行了拓展。我们的结构可以同时提供多个周期性的耦合系数，同时满足不同通道的滤波要求。

## Slide 42
超构材料多通道滤波器
多通道仿真的能量分布
同时实现了多个通道的滤波
损耗很低，小于0.8 dB.
旁瓣抑制比 >10 dB.
通道间串扰 <−25 dB
同时实现了多个通道的滤波
损耗很低，小于1 dB.
旁瓣抑制比 >20 dB.
通道间串扰< −30 dB
多通道仿真的频率响应

## Slide 43
超构材料多通道滤波器
实验结果：
损耗 < 1.5 dB
损耗 < 1.2 dB
通道间串扰 < − 19.2 dB
损耗 < 2 dB
通道间串扰 < − 14.3 dB

## Slide 44
超构材料多通道滤波器
实验结果(热调)：
单通道：
两通道：

## Slide 45
超构材料多通道滤波器
实验结果(热调)：
四通道：
热调效率：
0.200 nm/mW
0.176 nm/mW
0.174 nm/mW
0.148 nm/mW
0.150 nm/mW
0.157 nm/mW
0.151 nm/mW
在进行热调时，多个通道同步移动

## Slide 46
结果比较与总结
结构 | 器件尺寸(μm2) | 插入损耗(dB) | 串扰(dB) | 带宽(nm) | 通道数
阵列波导光栅[1] | 550 × 3900 | ≈5 | ≈–25 | ≈5 | 4
多模干涉器[2] | 12 × 1210 | ≈2 | ≈–15 | ≈8.5 | 4
马赫-曾德尔干涉仪[3] | 100 × 300 | ≈1 | ≈–18 | ≈16 | 4
光栅辅助反向耦合器[4] | 2 × 600 | ≈1 | ≈–11 | ≈12 | 4
多模波导光栅结构[5] | 40 × 600 | ≈1 | ≈–18 | ≈15 | 4
本工作 | 1.5 × 95 | 1.5 | - | 18.1 | 1
本工作 | 2 × 150 | 1.2 | –19.2 | 13.2 | 2
本工作 | 2.5 × 250 | 2 | –14.3 | 5.6 | 4
[1] P. Pan, J. An, Y. Wang, J. Zhang, L. Wang, Y. Qi, Q. Han, X. Hu, Opt. Laser Technol. 2015, 75, 177.
[2] Y. Hu, R. M. Jenkins, F. Y. Gardes, E. D. Finlayson, G. Z. Mashanovich, G. T. Reed, Opt. Lett. 2011, 36, 4488.
[3] H. Xu, Y. Shi, IEEE Photonics Technol. Lett. 2017, 30, 169.
[4] W.Shi, et al., Opt. Express 2013, 21, 6733.
[5] D. Liu, M. Zhang, Y. Shi, D. Dai, IEEE Photonics Technol. Lett. 2020, 32,
我们设计的器件有着旗鼓相当的损耗、带宽、串扰，同时我们的器件具有较小的尺寸。
这种多波长、多模式同时控制的方案在光谱仪、非线性光学等领域有潜在的应用价值。

## Slide 47
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望
  多维光复用通信系统
  超构材料的其他应用

## Slide 48
超构材料辅助的多维复用片上光通信系统关键器件研究
模式阶数复用
波长复用
Mode-order (de)multiplexing
Multi-channel WDM (de)multiplexing
Y. Zhao, X. Guo,* et al. Opt. Lett. 45, 3797-3800 (2020).
Y. Zhao, X. Guo* et al., ECOC 2020, Tu2B-4.
Y. Zhao, X. Guo* et al., Laser & Photonics Rev., 2200005, (2022).
Mode-order conversion
偏振复用
Polarization filtering
Polarization (de)multiplexing
Y. Zhao, X. Guo* et al., Laser & Photonics Rev., 2300320, (2023).

## Slide 49
硅基超构多维复用系统
超构材料多维复用


精准调控和高效耦合
5模式×2偏振×16波长
高集成度和大通量
多维光复用技术可以成倍提高通信容量，满足日益增加的通信容量需求

## Slide 50
硅基超构多维复用系统
超构材料多维复用


精准调控和高效耦合
5模式×2偏振×16波长
高集成度和大通量
多维光复用技术可以成倍提高通信容量，满足日益增加的通信容量需求

## Slide 51
支持多模式阶数的偏振分束器
器件结构
利用波导中TE和TM模式有不同的有效折射率，可以将两种不同的偏振态分开
C. Sun, Y. Yu, Y. Ding, Z. Li, W. Qi, and X. Zhang, Photonics Research 8, 978 (2020).

## Slide 52
支持多模式阶数的偏振分束器
仿真结果
损耗< 0.5 dB
串扰< –12 dB
TE input
TM input

## Slide 53
超构材料多维复用


精准调控和高效耦合
5模式×2偏振×16波长
高集成度和大通量
多维光复用技术可以成倍提高通信容量，满足日益增加的通信容量需求
硅基超构多维复用系统

## Slide 54
模式 (解)复用器 [TE偏振态]
器件结构
仿真结果
采用计算机辅助的逆向设计优化算法，设计了支持5种模式阶数的(解)复用器
损耗<2.5 dB
串扰<–12 dB

## Slide 55
超构材料多维复用


精准调控和高效耦合
5模式×2偏振×16波长
高集成度和大通量
多维光复用技术可以成倍提高通信容量，满足日益增加的通信容量需求
硅基超构多维复用系统

## Slide 56
模式 (解)复用器 [TM偏振态]
器件结构
仿真结果
采用计算机辅助的逆向设计优化算法，设计了支持5种模式阶数的(解)复用器
损耗<2.5 dB
串扰<–12 dB

## Slide 57
超构材料多维复用


精准调控和高效耦合
5模式×2偏振×16波长
高集成度和大通量
多维光复用技术可以成倍提高通信容量，满足日益增加的通信容量需求
硅基超构多维复用系统

## Slide 58
偏振旋转器
器件结构
仿真结果
损耗<0.5 dB
串扰<–17 dB

## Slide 59
超构材料多维复用


精准调控和高效耦合
5模式×2偏振×16波长
高集成度和大通量
多维光复用技术可以成倍提高通信容量，满足日益增加的通信容量需求
硅基超构多维复用系统

## Slide 60
波长解复用器
器件结构
仿真结果
反射的高阶模式可以通过模式解复用器耦合到不同通道
入射光在不同波长会反射回不同的模式中

## Slide 61
波长解复用器
O13
O14
O15
O16
16个通道可以通过四个四通道波长解复用器级联来进行设计
级联结构
预期结果

## Slide 62
系统架构
5模式×2偏振×16波长 = 160 通道
假设其他条件不变，预期可以通过160个通道实现21.62 Tbit/s的数据传输速度 [40 GBaud × 4 bits per symbol × 160 Channels × 97.1% / (1 + 15%)]。
16个模式通道
通过16个模式通道，传输40-GBaud 16 QAM信号的FEC低于15%，因此可以在单波长上实现2.162 Tbit/s的数据传输速度 [40 GBaud × 4 bits per symbol × 16 modes × 97.1% / (1 + 15%)]
Y. He, X. Guo, Y. Su, et al., Advanced Photonics 5, 056008 (2023).

## Slide 63
实验加工和测试
模式（解）复用器和偏振分束器实验加工已完成，正在进行测试中

## Slide 64
工作总结-硅基超构多维光场调控
硅基超构偏振调控
硅基超构模式调控
硅基超构波长调控
硅基超构多维复用系统
160通道多维光通信系统
迄今为止最小尺寸的模式阶数转化器和(解)复用器
超紧凑高性能偏振调控器件：起偏器、偏振分束器、偏振分束旋转器
多波长多模式同时调控，超紧凑波长(解)复用器
Y. Zhao, X. Guo,* et al. Opt. Lett. 45, 3797-3800 (2020).
Y. Zhao, X. Guo* et al., ECOC 2020, Tu2B-4.
Y. Zhao, X. Guo* et al., Laser & Photonics Rev., 2200005, (2022).
Y. Zhao, X. Guo* et al., Laser & Photonics Rev., 2300320, (2023).
To be continue.
Notes: This slide shows the schematics of the devices.

## Slide 65
目录
背景简介
超构材料光场调控机理
超构材料偏振调控
超构材料模式调控
超构材料波长调控
总结与展望
  多维光复用通信系统
  超构材料的其他应用

## Slide 66
超构材料赋能的可重构计算光谱仪
通过超构材料结构设计光谱响应，进一步提高可重构计算光谱仪的性能
B. Redding, S. F. Liew, R. Sarma, and H. Cao, Nature Photonics 7, 746 (2013).
W. Hartmann, P. Varytis, et al., Advanced Optical Materials 8, (2020).
A. Li, F. Bao, Y. Wu, et al., Laser & Photonics Reviews, 2301107 (2024).
W. Hartmann, P. Varytis, et al., Nano Letters, 20, 2625 (2020).
A. Li and Y. Fainman, Nature Communications 1 (2021).
X. Cai, J. Xiong, et al., arXiv:2005.02689v2.(2020).

## Slide 67
超材料赋能的非线性光学
通过超构材料提供的等效动量来调控非线性过程中的相位匹配，通过超构材料的谐振与慢光来增强非线性响应。
Y. Yang, L. Sun, Y. Zhang, and Y. Su, Advanced Optical Materials 7, 1 (2019).
C. Wang, Z. Li, et al., Nature Communications 8, 2098 (2017).
B. Corcoran, C. Monat, et al., Nature Photonic 3, 206 (2009).
J. R. Stone, X. Lu, et al., Nature Photonic. (2023).

## Slide 68
基于非线性效应的计算光谱仪
可以实现超紧凑(16×16 μm2)、低成本（无需额外光探测器）、低损耗的计算光谱仪
基于简单的微环调制器，通过双光子吸收的非线性效应将光信号转化为电信号
通过光谱重构方法用电信号重构入射光谱
Yaotian Zhao,† Xuhan Guo, *,† et al., Optica, vol. 11, no. 3, pp. 399-402, 2024.

## Slide 69
基于非线性效应的计算光谱仪
超紧凑 - 尺寸：16×16 μm2
低成本: CMOS兼容，工艺简单
暗电流低(0.1 nA), 灵敏度较差(1mA/W)
Type | Responsivity | Dark Current | Ref.
Lateral Ge PIN | < 1.14 A/W | <120 nA | [1]
Lateral Ge PIN | 1.06 A/W | ~500 nA | [2]
Lateral Ge PIN | 1.16 A/W | ~200 nA | [3]
Vertical Ge PIN | 0.95 A/W | 10 nA | [4]
Vertical Ge PIN | 1.09 A/W | 3.5 μA | [5]
This work（TPA） | 1 mA/W | 0.1 nA | -
[1] Y. Zhang, S. Yang, et al., Optics express 22, 11367–11375 (2014). [2] S. Lischke, D. Knoll, C. Mai, et al., Optics express 23, 27213–27220 (2015). [3] L. Virot, D. Benedikovic, et al., Optics Express 25, 19487–19496 (2017). [4] S. Liao, N.-N. Feng, et al., Optics Express 19, 10967–10972 (2011). [5] M. M. P. Fard, G. Cowan, et al., Optics Express 24, 27738–27752 (2016).
性能比较

## Slide 70
攻读博士期间发表论文
国际期刊：
Yaotian Zhao,† Xuhan Guo, *,† Jinlong Xiang, Zhenyu Zhao, Yujia Zhang, Xi Xiao, Jia Liu, Daigao Chen, and Yikai Su, "Miniaturized computational spectrometer based on two-photon absorption," Optica, vol. 11, no. 3, pp. 399-402, 2024.
Yaotian Zhao, Jinlong Xiang, An He, Yu He, Xuhan Guo,* and Yikai Su ,"Metamaterial-enabled fully on-chip polarization-handling devices," Laser & Photonics Reviews, no. 2300320, 2023.
Yaotian Zhao, Jinlong Xiang, Yu He, An He, Yong Zhang, Xuhan Guo,* Zongyin Yang, and Yikai Su, "On-chip metamaterial enabled wavelength (de)multiplexer," Laser & Photonics Reviews, no. 2200005, 2022.
Yaotian Zhao, Xuhan Guo,* Yong Zhang, Jinlong Xiang, Kangnian Wang, Hongwei Wang, and Yikai Su, "Ultra-compact silicon mode-order converters based on dielectric slots," Optics Letters, vol. 45, no. 13, pp. 3797-3800, 2020.
国际会议：
Yaotian Zhao, Jinlong Xiang, Yu He, Xuhan Guo, and Yikai Su, ECOC 2020, Tu2B-4.
Yaotian Zhao, Xuhan Guo, and Yikai Su, ACP 2020, M4A.178.
Yaotian Zhao, Xuhan Guo, Kangnian Wang, Hongwei Wang, and Yikai Su, ACP 2019, M3D.4.

## Slide 71
谢 谢！
https://otip.sjtu.edu.cn/

## Slide 72
实验加工和测试
单端损耗 < 3 dB
串扰< -10 dB
TM (DE)MUX
To be continue...

## Slide 73
Light: perception from human
Ref. The Electromagnetic Spectrum - Chemistry LibreTexts
Spectroscopy
Astronomy, Biology, and Chemical analysis…

## Slide 74
Chemical Spectra:
Detecting Material Composition
(e.g. Diabetes: Glucose concentration in blood or saliva-Absorption band of the fundamental vibrations of -CH, -NH, and -OH functional groups)
K. B. Bec, J. Grabska, and C. W. Huck, Molecules 25, 2948 (2020).
Stellar Spectra: Investigating Celestial Chemistry
Environmental Spectra: Monitoring Environmental Conditions
J. B. Kaler, Stars and their spectra: an introduction to the spectral sequence(Cambridge University Press, 2011).
https://muonray.blogspot.com/2016/08/nir-environmental-vegetation-monitoring.html
Applications

## Slide 75
Applications
Chemical Spectra:
Detecting Material Composition
Stellar Spectra: Investigating Celestial Chemistry
https://chemistrytalk.org/spectrophotometer-chemistry-instrument/
NASA’s Webb Telescope has yet another discovery machine aboard
– the Near-Infrared Spectrograph’s (NIRSpec’s) microshutter array.
From: https://webbtelescope.org/contents/media/images/2022/035/01G7HRYVGM1TKW556NVJ1BHPDZ
Notes: 不同的化学基团有不同的特征吸收光谱，可以用来识别待测材料的化学成分
不同的星系也有不同的发射光谱，可以用来做天文学的分析和拍照

## Slide 76
Applications
Environmental Spectra: Monitoring Environmental Conditions
https://muonray.blogspot.com/2016/08/nir-environmental-vegetation-monitoring.html
From Wikipedia
J. N. Apell and K. McNeill, Environmental Science: Processes & Impacts 21, 427–437 (2019).
Updated and validated solar irradiance reference spectra for estimating environmental photodegradation rates
Notes: 不同的大气组份对太阳光有不同的特征吸收峰，不同的温度也会有不同的红外光谱，通过卫星或无人机携带的光谱探测器可以识别环境组分，实现对环境的实时监测。

## Slide 77
Spectrometer
Z. Yang, T. Albrow-Owen, W. Cai, and T. Hasan, Science 371, (2021).
Conventional methods:
Challenges:
Wide Bandwidth
High Sensitivity
Low Cost
Small Size
High Resolution
Notes: 传统的光谱仪方案

## Slide 78
Pros: Low Cost, Small Size, High Sensitivity
Spectrometer
Emerging Trends
﻿Circumvent these performance limitations by advanced algorithms to deconvolute the interaction of incident light with spectral encoders with unique, varied spectral response characteristics
“Reconstructing” the original spectrum rather than directly measuring it.
Z. Yang, T. Albrow-Owen, W. Cai, and T. Hasan, Science 371, (2021).
﻿Data detection
Compressed Sensing
Reconstruction
Reconstructive method:
Cons: Instability
Notes: 最新出现的计算光谱仪的方案

## Slide 79
Spectrometer with multi-channels
Calculating Spectral Information from Signals Detected at Different Ports
B. Redding, S. F. Liew, R. Sarma, and H. Cao, Nature Photonics 7, 746 (2013).
Z. Yang, T. Albrow-owen, et al., Science 1020, 1017 (2019).
Resolution: 0.75 nm，Bandwidth: 25 nm
Footprint: 50 µm × 25 µm
Resolution: 15 nm，Bandwidth: 130 nm
Footprint:~50 µm ×20 µm
﻿Single nanowire broadband detector array
﻿Disordered Photonics
A. Li, F. Bao, Y. Wu, et al., Laser & Photonics Reviews, 2301107 (2024).
Resolution: 0.12 nm，Bandwidth: 120 nm
Footprint < 4 mm2
﻿Sensing optical power at different ports with PD
Reconstruct the spectrum from the sensed current
﻿Sensing optical power at different probes
Reconstruct the spectrum from the sensed current
﻿Sensing optical power at different ports with PD
Reconstruct the spectrum from the sensed current
Inverse designed SWG waveguide
Notes: 每个要有基本的作用原理，图不用太大，再排布一下
从不同端口来检测

## Slide 80
Spectrometer with multi-channels
W. Hartmann, P. Varytis, et al., Nano Letters, 20, 2625 (2020).
A. Li and Y. Fainman, Nature Communications 1 (2021).
X. Cai, J. Xiong, et al., arXiv:2005.02689v2.(2020).
Resolution: 4 nm，Bandwidth: 50 nm
Footprint: 200 µm × 100 µm
Resolution: 0.45 nm，Bandwidth: 180 nm
Footprint: 35 µm × 260 µm
Resolution: 0.8 nm，Bandwidth: 300 nm
Footprint: 7740 µm × 6330 µm
Calculating Spectral Information from Signals Detected at Different Ports
Stratified waveguide filters
﻿Disordered Photonics
Metasurface + CMOS Camera
﻿Sensing optical power at different ports with PD
Reconstruct the spectrum from the sensed current
﻿Sensing optical power at different ports with PD
Reconstruct the spectrum from the sensed current
﻿Sensing optical power at different pixel from the bottom CMOS image sensor
Reconstruct the spectrum from the sensed current
Notes: 每个要有基本的作用原理，图不用太大，再排布一下

## Slide 81
Spectrometer with different states
Calculating Spectral Information from Signals Detected in Different Device States
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, Optica 10, 1177 (2023).
C. Sun, Z. Chen, et al., Laser & Photonics Reviews 2200792 (2023).
J. Zhang, Z. Cheng, J. Dong, et al., Optica 9, 517 (2022).
Resolution: 0.005 nm，Bandwidth:100 nm
Footprint: 1000 µm × 1500 µm
Resolution: 0.36 nm，Bandwidth:16 nm
Footprint: 18 µm × 18 µm
Resolution: 0.2 nm，Bandwidth:20 nm
Footprint: 200 µm × 200 µm
Tunable cavity
Tunable nanobeam
Tunable microdisk
﻿Sensing optical power at the output port under different temperature (Heater voltage bias) by a power meter (off-chip)
Reconstruct the spectrum from the sensed optical power
Notes: 每个要有基本的作用原理，图不用太大，再排布一下
在不同的温度下进行检测

## Slide 82
Spectrometer with different states
Calculating Spectral Information from Signals Detected in Different Device States
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, Light: Science & Applications 12, 64 (2023).
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, ACS Photonics 10, 654 (2023).
Resolution< 0.08 nm，Bandwidth > 100 nm
Footprint: 20 µm × 35 µm
Resolution< 0.04 nm，Bandwidth > 100 nm
Footprint: 60 µm × 60 µm
C. Yao, M. Chen, T. Yan, et al., Light: Science & Applications 12, 156 (2023).
Resolution: 0.03 nm，Bandwidth:115 nm
Footprint: 2000 µm × 7600 µm
Tunable cascaded microrings
Tunable multimode microring
Tunable microring with MZI
﻿Sensing optical power at the output port under different temperature (Heater voltage bias) by a power meter (off-chip)
Reconstruct the spectrum from the sensed optical power
Notes: 每个要有基本的作用原理，图不用太大，再排布一下

## Slide 83
Reconstruction Algorithm
Advanced algorithms can be further utilized for the analysis and reconstruction of spectral information
Z. Yang, T. Albrow-Owen, W. Cai, and T. Hasan, Science 371, (2021).
Calibration process:
Obtain at different channel and different wavelength with a known spectrum input.
Detection process:
Measure at different channel with the target spectrum.
Reconstruction process:
Reconstruct target spectrum from .
N : discrete heating power/Channels
M : wavelength band（points)
Notes: 在calibration的process中，通过单波长激光器获得系统在不同波长，和不同检测通道下，的响应
在检测的过程中，检测不同通道下的响应电流
For the computational reconstruction process, a response matrix T, with Np rows, each corresponding to a discrete heating power, and Mw columns, each corresponding to a wavelength band, is pre-calibrated by measuring transmission spectra in the output port while linearly sweeping the external heating power. If the unknown incident signal I with Mw wavelength points pass through the PM spectrometer, the spectral information can be sampled and encoded, along with the detected output power S with Np heating channel number recorded. S can be mathematically expressed as a vector product:
█(𝑺_(𝑁_𝑝×1)=𝑻_(𝑁_𝑝×𝑀_𝑤 ) 𝑰_(𝑀_𝑤×1)#(5) )
By measuring Np optical powers, where Np is far less than the Nyquist frequency (Np≪ Mw), a signal with Mw wavelength points can be reconstructed. By solving this inverse problem via a reconstruction algorithm (see Methods), we can arrive at an approximation of I.

## Slide 84
Data Detection Method
Collecting Spectral Signals Data through Various Methods
X. Cai, J. Xiong, et al., arXiv:2005.02689v2.(2020).
Z. Yang, T. Albrow-owen, et al., Science 1020, 1017 (2019).
Other Material
S. Yuan, D. Naveh, K. Watanabe, T. Taniguchi, and F. Xia, Nature Photonics (2021).
Off-Chip Power Meter
J. Zhang, Z. Cheng, J. Dong, et al., Optica 9, 517 (2022).
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, ACS Photonics 10, 654 (2023).
Camera
B. Redding, M. Alam, M. Seifert, and H. Cao, Optica 1, 175 (2014).
Black phosphorus photodetector
﻿All-fiber spectrometers+Camera
Metasurface units + Camera
Notes: 每个要有基本的作用原理，图不用太大，再排布一下
用不同的方法来探测光信号，
第一个是用CMOS image sensor, 就是红外相机在每个像素点上探测光信号强度
第二个是用片外的光功率计来探测光信号强度
第三个是用片上的异质材料，他们对不同的光有不同的电流响应，来探测光信号强度。

## Slide 85
The physical properties of resonators
Notes: 谐振腔对光波长有着非常好的选择作用
因此光信号波长的微小变化可以灵敏的反应到测试得到的信号中

## Slide 86
Our method: TPA detector->No PD!
In the process of two-photon absorption, two photons are absorbed to generate electron-hole pairs.
The generated free carriers can be characterized through the current signal in a reverse-biased PN junction.
T. K. Liang, H. K. Tsang, et al., Applied Physics Letters 81, 1323 (2002).
Y. Ren, V. Van et al., IEEE Journal of Selected Quantum Electronics, 26,3 (2020)
M. Casalino, et al., Laser & Photonics Reviews 10, 895–921 (2016).
Notes: 这部分再找找文献，把TPA原理讲透。可以参考LPR- Casalino - State‐of‐the‐art all‐silicon sub‐bandgap photodetectors at telecom and.pdf

## Slide 87
Our method: TPA detector->No PD!
T. K. Liang, H. K. Tsang, et al., Applied Physics Letters 81, 1323 (2002).
Y. Ren, V. Van et al., IEEE Journal of Selected Quantum Electronics, 26,3 (2020)
﻿PDs ：Single-photon absorption typically require Ge on silicon, SiGe or defect implantation.
Si PDs based on two-photon absorption (TPA): do not require extra fabrication steps beyond the standard CMOS process and are thus more cost-effective and easier to incorporate into Si PICs.
Notes: 这部分再找找文献，把TPA原理讲透。可以参考LPR- Casalino - State‐of‐the‐art all‐silicon sub‐bandgap photodetectors at telecom and.pdf

## Slide 88
Principle of TPA detector
Collecting spectral information through two-photon absorption is a fully CMOS-compatible method, featuring advantages such as low dark current, small size, low cost, and low optical loss.
However, with relative poor responsivity (3 orders)->Enhanced in Microring resonator!
Type | Responsivity | Dark Current | Ref.
Lateral Ge PIN | < 1.14 A/W | <120 nA | [1]
Lateral Ge PIN | 1.06 A/W | ~500 nA | [2]
Lateral Ge PIN | 1.16 A/W | ~200 nA | [3]
Vertical Ge PIN | 0.95 A/W | 10 nA | [4]
Vertical Ge PIN | 1.09 A/W | 3.5 μA | [5]
Our TPA work | 1 mA/W | 0.1 nA | #
[1] Y. Zhang, S. Yang, et al., Optics express 22, 11367–11375 (2014).
[2] S. Lischke, D. Knoll, C. Mai, et al., Optics express 23, 27213–27220 (2015).
[3] L. Virot, D. Benedikovic, et al., Optics Express 25, 19487–19496 (2017).
[4] S. Liao, N.-N. Feng, et al., Optics Express 19, 10967–10972 (2011).
[5] M. M. P. Fard, G. Cowan, et al., Optics Express 24, 27738–27752 (2016).
# Y. Zhao,† X. Guo,†, * Y. Zhang, Y. Su, et al., Optica 11, 399 (2024).
Pre-equalization of the nonlinearity:
Get the real TPA current response from real measurement.
T. K. Liang, H. K. Tsang, et al., Applied Physics Letters 81, 1323 (2002).
Notes: 这部分精简

## Slide 89
TPA based computational spectrometer
TPA current Iph,N×1 is obtained by direct measurement at different channels.
Data Sampling:
Spectral Reconstruction:
The target spectrum S2M×1 ​is calculated by solving the matrix.
The sampling matrix γN×M​ is obtained through a calibration at different channels and different wavelength.
Computational spectrometer
Linear regression algorithm is utilized to solve the matrix by minimizing l2​ norm
​
Notes: 这部分精简

## Slide 90
Experimental Result
Experimental setup
TPA responses with different heater power and wavelength
TPA current is much larger at resonant wavelengths
Thermal tuning process changes the resonant wavelength
TPA responses with different optical power and wavelength
Larger the incident light, Larger TPA current
Measured response
Notes: 再想想这个如何排布和如何讲

## Slide 91
Experimental Result
Computing the autocorrelation of the sampling matrix
Resolution of the spectrometer is estimated to be 0.32 nm.
Y. Zhao,† X. Guo,†, * Y. Zhang, Y. Su, et al., Optica 11, 399 (2024).

## Slide 92
Experimental Result
Computation spectrometer
Spectral Generation: Utilize ASE and TSL to generate spectral signals
Data detection: Use one current source to thermally tune the micro-ring and another current source to sample the current
Spectral Reconstruction: Reconstruct spectra with both wide spectral bandwidth and narrow linewidths.
Resolution
0.4 nm
Bandwidth
10 nm
Y. Zhao,† X. Guo,†, * Y. Zhang, Y. Su, et al., Optica 11, 399 (2024).
,

## Slide 93
Comparison
Performance
Footprint：16×16 μm2
Resolution：0.4 nm
Bandwidth：10 nm
Features：
1. PD free
2. Low optical loss
3. Low cost
Y. Zhao,† X. Guo,†, * Y. Zhang, Y. Su, et al., Optica 11, 399 (2024).

## Slide 94
Bandwidth enhancement
The bandwidth is enhanced by cascaded multiple MRRs with more information.
The bandwidth is demonstrated to 30 nm by cascading three MRRs.

## Slide 95
Resolution
The TPA current is proportional to the square of the incident light energy
The PD current is proportional to the incident light energy.
TPA current has a shaper response, thus has a better resolution for the same design.

## Slide 96
Noise & Sensitivity
The signal-to-noise ratio of the TPA current is approximately around 2000
The dark current increases with the rise in thermal tuning temperature
The energy entering the system needs to be greater than -10 dBm.
Further increasing the Q-factor can enhance the sensitivity of the spectrometer.
SNR at different reverse-biased PN junction voltages
The dark current at different thermal tuning powers
The sensed current at different input optical power

## Slide 97
Bandwidth limitation
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, Light: Science & Applications 12, 64 (2023).
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, ACS Photonics 10, 654 (2023).
The FSR in resonator limits the bandwidth
Computational spectrometer using a multimode MRR or cascaded MRRs
Provide different response in different FSR
Achieve a wide bandwidth (>100 nm) -> Break the FSR limitation!

## Slide 98
Resolution and Sensitivity
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, ACS Photonics 10, 654 (2023).
Q = 4.4×104，Resolution< 40 pm
The Q factor in resonator limits the resolution
H. Xu, Y. Qin, G. Hu, and H. K. Tsang, Light: Science & Applications 12, 64 (2023).
Q = 2×104，Resolution< 80 pm
Increase Q
The resolution primarily depends on the response to wavelength variations and the noise of the system.
Increasing the Q-factor and optical packaging can contribute to improving the resolution.
Increasing the Q-factor also enhances nonlinear effects, thereby improving the sensitivity.

## Slide 99
Three-body problems
Newton,1687
Predictable
Chaotic
Solar System
Randomness

## Slide 100
Disordered Photonic Molecule Spectrometer
*Manuscript in revision
> 7.74×105

## Slide 101
Performance
Performance
Footprint：70×50 μm²
Resolution：8 pm
Bandwidth：>100nm
Features：
Surpasses the “resolution-bandwidth-footprint” metric of current spectrometers
*Manuscript in revision

## Slide 102
Outlook
Further advancements can be made by utilizing high-Q cascaded MRRs or Microdisk Photonic molecules, employing broadband edge couplers, incorporating optoelectronic packaging, and integrating temperature controller. This approach enables low cost, high resolution, large bandwidth, and high sensitivity for the spectrometer system.
Y. Zhao,† X. Guo,†, * Y. Zhang, Y. Su, et al., Optica 11, 399 (2024).

## Slide 103
Outlook
Applications:
Cellphone Spectrometer
C. Zhang, et al., Lab on a Chip 16, 246 (2016).
G-Fresnel smartphone spectrometer
Spectrometer chip
Ultra-portable, wireless smartphone spectrometer for rapid, non-destructive testing of fruit ripeness
A. J. Das, et al., Scientific reports 6, 32504 (2016).
Sensing and monitoring
From PASCO
Chemical Analysis

## Slide 104
Thank you!
Fundings:
Optical Transmission and Integrated Photonics (OTIP)
National Key R&D Program of China (2021YFB2801903, 2023YFB2804702)
Natural Science Foundation of China (NSFC) (6217515)
Shanghai Municipal Science and Technology Major Project
http://otip.sjtu.edu.cn
Collaborators:
Yaotian Zhao
Yujia Zhang
PhD students involved:
Prof. Tawfique Hasan,
Cambridge University
Acknowledgements
Prof. Zongyin Yang,
Zhejiang University